[image: image1.png]/7 T\\N\
RENEWABLE
LUBRICANT Se




Renewable Lubricants, Inc.
     476 Griggy Rd., P.O. Box 474

      Hartville, Ohio 44632-0474

      330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com

ReNu Source™ Oils
(ISO- 32, 46, 68, 100, 150, 220, 320, 460, 680, 1000,1500, 3000)

ReNu Source™ Oils are produced from high oleic base stocks (HOBS) and synthetic polyol esters.  HOBS are renewable high oleic natural esters that have improved oxidation stability over conventional biobased oils produced from animal and plants.  In addition to available Natural Based oils (NBO) high in oleic content. ReNu Source™ Oils have been produced in different viscosities by combining Natural Based oils (NBO) with Renewable Synthetic based Polyol Esters (see data below for (RSPE).  ReNu Source™ Oils RSPE and NBO are additive free and may be used by compound blenders for improving formulations in many industrial applications.  They offer high biodegradability and low toxicity in aquatic conditions and can be used in formulating biobased products for environmentally sensitive areas such as in agriculture, forestry and marine.  ReNu Source™ Oils provide excellent compatibility with the same seals and components that are designed to operate on petroleum oil based formulas.  As an additive, or primary base oil, their natural oiliness has shown to provide additional lubricity in engine oils, hydraulic fluids, gear oils, and many metal working fluid/oil applications. The super high viscosity index and heavy viscosities of these biobased esters naturally provides additional fluid film value at the higher temperatures, which is a performance benefit over lower VI products of the same viscosity.  This super high viscosity index improves the thermal shear stability of any formula, increases load capacity in the contact zone, reduces wear, and provides for energy conserving formulations.  Their extremely low volatility increases the flash and fire safety features in the formula.
Applications:  for formulating Metal Working Fluids, Greases, Gear Oils, Hydraulic Fluids, Drip Oils, Air-Oils, Air-Tool Oils, Machine Oils, Chain and Cable Oils, Wire Rope Oils, Circulating Oils, and many General-Purpose Lubricants, etc.

The advantages are many:  biodegradable, renewable, low toxicity, no volatile organic compounds (VOCs), safer, more fire resistant, provides for EPA and ISO 14000 compliance, reduces foreign oil, and helps secure the American Economy. OSHA and worker acceptance are high with biobased oils.

Typical Specifications
	Type Base Oil
	POE
	RSPE
	RSPE
	RSPE
	RSPE
	RSPE
	RSPE
	RSPE
	RSPE
	RSPE
	RSPE

	ISO Grade 
	22
	22
	32
	46
	68
	100
	150
	220
	1000
	1500
	3000

	ASTM Grade (Neutral Oil) 
	100
	100
	150N
	215N
	315N
	465N
	700
	1000N
	4650
	7000
	----

	Spec. Gravity @ 60OF. (D-287)
	1.002
	.90
	.90
	.91
	.92
	.92
	.95
	.96
	.97
	.99
	.99

	VISCOSITIES:
	
	
	
	
	
	
	
	
	
	
	

	  @100OC., cSt. (D-445)
	4.4
	5.2
	7.18
	9.93
	13.05
	18.0
	26.9
	32
	110
	155
	268

	@40OC., cSt. (D-445)
	19
	21
	31.28
	45.67
	61.52
	91.0
	139.52
	199
	920
	1460
	3200

	Viscosity Index (D-2270)
	133
	195
	205
	213
	218
	218
	216
	206
	220
	222
	160

	Flash Point, COC, OC (D-92)
	250
	245
	280
	290
	280
	280
	280
	290
	290
	300
	310

	Pour Point, OC (D-97)
	-55
	-30
	-25
	-21
	-22
	-25
	-15
	-16
	-18
	-20
	-27

	Copper Corrosion ASTM D-130
	1B
	1B
	1B
	1B
	1B
	1B
	1B
	1B
	1B
	1B
	1B

	Rust Prevention (D-665 A
	Pass
	Pass
	Pass
	Pass
	Pass
	Pass
	Pass
	Pass
	Pass
	Pass
	Pass

	Biodegradability ASTM-5864/7373%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%

	Biodegradability OECD 301B %
	>75
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%

	Meets and exceeds EPA VGP EAL
	yes
	yes
	yes
	yes
	yes
	yes
	yes
	yes
	yes
	yes
	yes

	USDA Biobased %
	>75
	78%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%
	>60%

	RLI Product Item #
	79200
	79100
	79110
	79120
	79130
	79140
	79150
	79160
	79170
	79180
	79190


Polyol Esters (POE) plus Natural HOBS Based oils (NBO),=  ReNu Source™ Oils RSPE
ReNu Source™ Oils meet the Environmental Protection Agency (EPA) Vessel General Permit (VGP) guidelines for formulating Environmentally Acceptable Lubricants (EALs), and should be used in formulations where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  They exceed the acute toxicity (LC-50 / EC-50 >1000 = ppm1000mg/L) criteria adopted by the US Fish and Wildlife Service and the US EPA.  ReNu Source™ Oils are ENVIRONMENTALLY RESPONSIBLE base oils that are produced from renewable agricultural biobased resources.  We believe Earth’s environmental future rests in the use of renewable material.

1Ultimate Biodegradation Pw1 >60% within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants
* Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.
Availability
F.O.B.: Hartville, Ohio, USA      Drum   Totes   Bulk

