[image: image1.jpg]STABILIZED "

Renewable Lubric



Renewable Lubricants, Inc.
476 Griggy Rd., P.O. Box 474

Hartville, Ohio 44632-0474

Voice:  330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com

[image: image2.png]


[image: image3.png]/7 T\\N\
RENEWABLE
LUBRICANT Se



Bio-SynXtra™ Hydrostatic Fluid 
(Low-Viscosity) Universal Tractor Fluid

"Biobased Lubricants that 
Perform Like Synthetics"
Bio-SynXtra™ Hydrostatic Fluid is a universal tractor fluid that incorporates Stabilized* additive technology with biodegradable vegetable based stocks.  This formulation contains special frictional modifiers for the Wet Brake’s equipment design, and is compounded with detergent, dispersant, anti-wear, anti-rust, and anti-foam inhibitors.  This Bio-SynXtra™ Hydrostatic Fluid is an ultimately biodegradable1, multi-grade lubricant that can be used in agricultural, industrial and construction equipment where low viscosity and improved cold-temperature performance is required.

Bio-SynXtra™ Trans-Hydraulic Fluid has been highly tested, Tractor Life.com Authenticated, and can be used to meet or exceed all of the following performance specifications of: Massey-Ferguson M-1110, Ford-New Holland M2C41-B, and Case-IH MS 1210.  Approved or Recommended in Allison C-3 and Cat TO-2.  Meets or exceeds ISO-32 Hydraulic for Vickers, Denison, Commercial Intertech, Rexroth, Sauer-Sundstrand, and API GL-4 gear requirements for low viscosity fluid applications.
Kinematic Viscosity ASTM D-445

@40°C = 31.0 cSt

@100°C = 7.3 cSt

Viscosity Index ASTM D-2270

213

Specific Gravity ASTM D-287

@15.5°C = .879

Pounds per Gallon 

7.32
Cleveland Open Cup ASTM D-92

Flash Point °F/°C = 385/196

Fire Point °F/°C   = 415/215
Pour Point ASTM D-97
<-45°C

ASTM D-974

Total Acid Number = 0.56
Brookfield Viscosity (cP) 
@-40°C = <20,000 cP

Dielectric Strength (ASTM D-877)

48 KV

(Before use:  Use oil viscosity based on the expected temperature range specified by OEM)

Bio-SynXtra™ Hydrostatic Fluid meets the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used in hydraulic systems where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  This product exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-SynXtra™ Hydrostatic Fluid is an ENVIRONMENTALLY ACCEPTED LUBRICANT (EAL) that is formulated from renewable, agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable materials.
1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants
STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.
Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.   Copyright 1999 Renewable Lubricants, Inc.

Availability
F.O.B.: Hartville, Ohio, USA    1 Gallon  5 Gallon Pail    Drum     Totes      Bulk

RLI Product Item # 


            81303
  81304            81306     81307     81309

