[image: image1.jpg]STABILIZED "

Renewable Lubric





Renewable Lubricants, Inc.
     476 Griggy Rd., P.O. Box 474

      Hartville, Ohio 44632-0474

      330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com


[image: image2.png]/7 T\\N\
RENEWABLE
LUBRICANT Se




Bio-Vacuum Pump™ Oil  ISO 46, 68, 100
"Biobased Lubricants that Perform Like Synthetics"

Bio-Vacuum Pump™ Oil is an ultimately biodegradable1 biosynthetic formula that is recommended in the dairy industry for automatic milking machines and most other vacuum pump applications.  It provides protection in vacuum pumps that require Anti-Wear (AW), anti-rust, anti-oxidation, anti-foam, and demulsibility properties.  Incorporating the super high viscosity index (VI) of the Stabilized* High Oleic Base Stocks (HOBS) into the formula, increases the viscosity index past synthetic levels (Energy Conserving Formulas).  The HOBS’s extremely low volatility increases the flash and fire safety features in the formula and reduces oil volatility.
Bio-Vacuum Pump™ Oil meet the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  It exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Vacuum Pump™ Oil is an ENVIRONMENTALLY RESPONSIBLE lubricant that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Typical Specifications
SAE Grade




10W30

30

100
ISO Grade




46

68

100
VISCOSITIES:

@100OC., cSt.



9.67

11.2

16.7
@40OC., cSt.



43.8

62.8

92.0
Viscosity Index




216

189

199
Flash Point, COC, OC.



243

248°C

255°C
Fire Point, COC, OC.



268

270°C

280°C
Pour Point, OC.




-36

-30

-34
Brookfield, @-25O C., cP, (D-2983)

3,000

4,500

5,400
MRV @ -30 O C, (TP-1)


8,000

15,000

26,00
Copper Corrosion Strip 3hr @ 100OC.

1B

1B

1A
4 Ball Wear, 1h, 167O F, 1200 RPM, 40kg
0.3-0.4

0.4

0.4
Demulsibility (D-1401)



40/40/0

40/40/0

40/40/0
Foam Sequence I, II, III (D-892)


0

0

0
Rust Prevention, (D-665 A&B)


Pass

Pass

Pass
Item#





84100

84110

84120
STABILIZED by Renewable Lubricants™* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high-performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability
F.O.B. :Hartville, Ohio, USA   Quart    1 Gallon    5 Gallon Pail    Drum   Totes    Bulk

