[image: image1.jpg]STABILIZED "

Renewable Lubric




Renewable Lubricants, Inc.
     476 Griggy Rd., P.O. Box 474

      Hartville, Ohio 44632-0474

      330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com

[image: image2.png]/7 T\\N\
RENEWABLE
LUBRICANT Se



Bio-Shredder™ Machine Lubricant

"Biobased Lubricants that Perform Like Synthetics"
Bio-Shredder™ Machine Lubricant is a blended highly refined vegetable based formula (Biobased) that replace neutral petroleum mineral oils in light machine applications. This product has been Stabilized* to resist oxidation and provide excellent light color stability and is Food Grade2.  It is virtually aromatic, chlorine, and sulfur free.  The base oil has been highly refined, bleached, deodorized and is high in oleic acid content for higher stability over conventional vegetable oils.  This product provides excellent compatibility with rubber, plastics, general purpose elastomers, and other materials that this product may be in contact with.  It provides excellent lubricity for recommended applications.

Bio-Shredder™ Machine Lubricant is a ENVIRONMENTALLY RESPONSIBLE base lubricant that is formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable material.

The advantages are many:  biodegradable1, renewable, low toxicity, no volatile organic compounds (VOCs), safer, more fire resistant, EPA and ISO 14000 compliant, reduces foreign oil, and helps secure the American Economy.  OSHA and worker acceptance is high with biobased oils.

Typical Specifications
API Gravity @ 60OF.




26.7

Pounds/Gallon @ 60OF.




7.45

Specific Gravity @60OF.




.89

VISCOSITIES:


@100OC., cSt. (D-445)



7.18

@40OC., cSt. (D-445)



31.28

Viscosity Index (D-2270)




205

Flash Point, COC (D-92)




260OC

Pour Point, OC (D-97)




-20

Copper Corrosion (D-130) 3hr @ 100OC


1A

Acid Number (D-974)




0.08

Foam Sequence I, II, III (D-892) 10 min.


0 Foam

Rust Prevention, (D-665 A)



Pass Clean

4 Ball Wear Scar Diam (mm) (D-4172)


.65

Biogradability 1 (D-5864) Pw1





    Yes

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

2 Base oils and additives in this product are listed in 21 CFR 178.3570, Lubricants for incidental food contact (USDA H-1).  Full compliance with other applicable restrictions of FDA, USDA, oil spill, and oil pollution prevention statutes is recommended.

Patented Product: US Patent 6,383,992, US Patent 6,534,454, US Patent 6,624,124, US Patent 6,620,772 with additional Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability
F.O.B. :Hartville, Ohio, USA           1 Gallon    5 Gallon Pail    Drum     Totes    Bulk

RLI Product Item #



                   87473
87474
            87476        87477     87479

