[image: image1.jpg]STABILIZED "

Renewable Lubric





Renewable Lubricants, Inc.
476 Griggy Rd., P.O. Box 474

Hartville, Ohio 44632-0474

Voice: 330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com

[image: image2.png]/7 T\\N\
RENEWABLE
LUBRICANT Se



Bio-MultiPurpose™ Machining Oils ISO 32, 46, 68

(Hydraulic Fluid, Gear Oil, Cutting Oil, Machine Lube)

"Biobased Lubricants that Perform Like Synthetics"

Bio-MultiPurpose™ Machining Oils are ultimately biodegradable1, biobased lubricants formulated with natural and synthetic base oils for light to medium-heavy duty machining operations.  They provide protection in today’s hi-tech machines operating at increased speeds and feed rates and their multipurpose performance helps in reducing inventory and lowering cost.  Their color can be classified as transparent, which permits viewing the cutting operations while in process and they are formulated to reduce smoke and mist.  Performance is enhanced by use of the *Stabilized HOBS’s, natural fatty acid composition, which provides cutting tool wetting and oiliness; combined with excellent extreme pressure and antiwear technology.  The super high viscosity index of the Stabilized HOBS adds additional lubrication qualities in industrial gear, hydraulic, and machine systems.  They are non-staining to yellow metals and may be used for machining both ferrous and non-ferrous metal alloys.  The products do not contain active sulfur, chlorine, zinc, silicon, or heavy metals, and do not produce an abrasive odor.

The advantages are many:  biodegradable, renewable, low toxicity, no hazardous volatile organic compounds (VOC), more fire resistant, safer, EPA and ISO 14000 compliant, reduces foreign oil, and helps secure the American Economy, OSHA and worker acceptance is high with biobased oils.

Bio-MultiPurpose™ oils are ENVIRONMENTALLY RESPONSIBLE lubricants that are formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable materials.
Typical Specifications
ISO Grade





32

46

68
Specific Gravity @60OF.




.90

.90

.90

VISCOSITIES:
  @100OC., cSt.



6.9

9.0

13.0


   @40OC., cSt.



32.5

45.6

67.0

Viscosity Index





182

184

199

Flash Point, COC OC




230

238

240

Pour Point, OC





-20

-18

-18

Copper Corrosion ASTM D-130



1B

1B

1B

Rust Prevention ASTM D-665 A&B


No Rust

No Rust

No Rust

Foam Sequence I, II, III (10 min) ASTM D-892

0 Foam

0 Foam

0 Foam

Demulsibility ASTM D-1401



40/40/0

40/40/0

40/40/0

4-Ball Wear ASTM D-4172 (mm)



.40

.40

.40


4-Ball EP Weld Pt. ASTM D-2783 (kg)


400

400

400



Load Wear Index




53

58

66


FZG  DIN 51354 Part 2




>12

>12

>12


RLI Product Item #




86930

86940

86950
STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents
 * Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability
F.O.B. :Hartville, Ohio, USA      1 Gallon   5 Gallon Pail    Drum  Totes  Bulk

