[image: image1.jpg]STABILIZED "

Renewable Lubric





Renewable Lubricants, Inc.
476 Griggy Rd., P.O. Box 474

Hartville, Ohio 44632-0474

Voice: 330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com

[image: image2.png]/7 T\\N\
RENEWABLE
LUBRICANT Se



Bio-Slide Way™ Lubricants
"Biobased Lubricants that Perform Like Synthetics"

Bio-Slide Way™ Lubricants are specially formulated biodegradable1, biobased products developed for the lubrication of machine tools and slides.  They eliminate stick-slip or table chatter by reducing friction between mating surfaces.  Where ways are heavily loaded they provide super high film strength and excellent EP protection.

Bio-Slide Way™ Lubricants formulations have metal wetting and adhesion properties that enable them to form uniform films that resist squeezing from way surfaces while machine is not in operation.  By preventing stick-slip, the wear of way surfaces is minimized and their service life is greatly extended.

Bio-Slide Way™ 32 Lubricant is generally recommended for dual purpose hydraulic and way lubrication service.

TYPICAL SPECIFICATIONS








32

68

220

Viscosity, cSt  /400 C

D-445

30.1

63

199


  cSt /1000 C

D-445

6.7

12.1

30

Gravity, 0API


D-287

30.3

27.8

25.3

Viscosity Index


D-2270

190

191

193

Rust, Syn. Sea Water

D-665B

PASS

PASS

PASS

Flash, COC 0C


D-92

256

273

290

Pour, 0C



D-97

-25

-25

-20

Timken OK Load, lb.

D-2782

60

60

60

4-Ball Load




    Wear Index, kg

D-2783

35.5

37.2

46.8

4-Ball Weld Point, kg

D-2783

200

200

250

Thermal Stability




PASS

PASS

PASS

Cincinnati Machine









        Spec. No.




P-53

P-47

P-50


Stick Slip




.72

.72

.72


RLI Product Item #



86900

86910

86920
STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

 * Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability
F.O.B. :Hartville, Ohio, USA      1 Gallon   5 Gallon Pail   Drum  Totes   Bulk

