[image: image1.png]/7 T\\N\
RENEWABLE
LUBRICANT Se



Renewable Lubricants, Inc.
476 Griggy Rd., P.O. Box 474

Hartville, Ohio 44632-0474

Voice: 330.877.9982  Fax  330.877.2266
Web: www.renewablelube.com

RLI E.P. 300 Lithium Multipurpose Grease

NLGI # 2
PRODUCT DESCRIPTION

RLI E.P. 300 Grease is a lithium 12 hydroxy lubricating grease formulated with the highest quality base oils available, and is fortified with rust and oxidation inhibitors as well as extreme pressure additives. This product has been formulated with a special additive package which insures high film strength, extreme pressure (EP) and anti-wear properties.

RECOMMENDED APPLICATIONS

For use in/on any of the following:

· Plain/rolling-element bearings 

· Compressors

· Fans

· Centrifugal pumps

· Chassis parts

· U-joints

· Water pumps on passenger cars

· Track Rollers

· Commercial lawn mowers

· General-purpose/shop/industrial grease

· Underground mining machinery

· Crushers

· Vibrating screens

· Centralized lubrication systems

PRODUCT BENEFITS

Has a variety of uses and is formulated with special additive to perform well under extreme pressure.
TYPICAL PROPERTIES

NLGI Grade 2

Thickener Type 






Lithium

Color 







Amber

Texture 







Buttery

Appearance 






Smooth

Operating Temperature Range 




-30°F to +250°F

Penetration 



ASTM D 217

Worked 60 Strokes @ 77 °F 




265-295

Dropping Point, °F (°C) 


ASTM D 2265 

350 (177)

Oil Separation, % Loss Max 


ASTM D 1742 

10

4 Ball Wear Test, mm Scar Diameter 

ASTM D 2266 

0.45

4 Ball E.P. Weld Point, 


ASTM D 2596 

250

4 Ball Load Wear Index, Kgf 


ASTM D 2596 

40

Water Washout, % Loss Max 

ASTM D 2509 

10

Timken Load Carrying Test of Grease Lbs. 
ASTM D 2509 

45

Rust Preventative Properties of Greases 
ASTM D 1743

Pass

Pressure Vessel Oxidation PSI Drop 

ASTM D 942 

5

Wheel Bearing Leakage, grams Loss 

ASTM D 4290 

5

Copper Corrosion of Greases 


ASTM D 4048 

1b

Base Oil Characteristics 


ASTM D 445

Viscosity @ 100°C cSt 




11.5-14.5

Viscosity @ 40°C cSt 




150-200

Viscosity Index






50
* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability
F.O.B. :Manufacturer
 14 oz. Tube    35 lb  Pail    120 lb Keg    400 lb Drum 

RLI Product Item #



         88921
   88924
          88925
    88926

